Method A - Application Guide

| Suitable for all metal surfaces including bronze, stainless steel and aluminium and is applied using heat as a penetration catalyst (Note that more detailed written instructions for both methods are included with your Propshield purchase along with further detailed precautions). WARNINGS: 1) Do not use Method A on painted surfaces, i.e. outdrive legs and outboards however you can use either method on your outdrive/outboard propellers if the blades on are bare metal. 2) Do not overheat outdrive/outboard props as the rubber insert/seals in some designs of prop hub can be damaged. If unsure check with the manufacturer of your outdrive or outboard motor. The below example/guide shows Propshield being applied to a bronze propeller |
| --- |
| STEP 1 Surface Preparation: First clean the metal surface | STEP 2 Heat the surface (in this case the propeller) with a blow lamp or heatgun |
| STEP 3 Now with a rag or brush wipe Propshield onto the propeller blade until a very thin film is applied | STEP 4 Once the first coat has been applied over the whole surface melt some Propshield into a metal container until it is a liquid. |
| STEP 5 Now dip a rag or brush into the liquid Propshield and apply a thicker coat to the blades | STEP 6 The job is now completed and the vessel is ready to launch |