Method B - Application Guide

| Suitable for painted surfaces as well as all metal surfaces and is applied using white spirit as a penetration catalyst (Note that more detailed written instructions for both methods are included with your Propshield purchase along with further detailed precautions). The below example/guide shows Propshield being applied to a bronze propeller. |
| --- |
| STEP 1 Surface Preparation: First clean the metal surface | STEP 2 Dissolve a small amount of Propshield into a plastic container with white spirit |
| STEP 3 On a rag wipe the Propshield & white spirit mixture onto the blade until a very thin film is applied | STEP 4 Again dilute Propshield with approximately 5% to 15% White Spirit (or melt Propshield with a heatgun or by dropping a tub of Propshield into a bowl/tub of hot water) |
| STEP 5 Now apply a second thicker coat; dip a rag into the liquid Propshield and apply a thicker coat to the blades | STEP 6 The job is now completed and the vessel is ready to launch. |